1-1-100 EXP WITH EXPANDING CEMENTING ADDITIVE GAS STOP PREVENTION CEMENT ADDITIVE KIT 1- Pail Additives, 1- Super Sack Cement, 100 - Gallons Fresh Water Field Data Sheet 1 Five gallon pail has pre-measured Fluid Loss, and Dispersant 1 Lehigh Class H Jumbo Sack (2000#) 100 Gallons Fresh Water Field Mixing Procedure Start with 100 gallons of Fresh Water in the tank for each Super sack of cement. Add the predetermined amount of DHS liquid retarder (from the Technical Data Sheet) and the 5 gallon bucket/buckets of pre-measured, dry additives and let them disperse. The order of addition does not matter for the retarder and the 5-gallon bucket of dry additives. Then slowly add bulk super sack/sacks (2000#) of cement. Anti-foaming additives may be added if needed. 1-1-CEMENT ADDITI Retarder Formula YIELDS 4.0 BBLS (128 oz’s = 1 gal) DENSITY 16.2 PPG Example @ 190 deg F 48oz / 128 = 0.375 gal YIELD 1.09 FRESH WATER 100 gallons Fresh TEMPERATURE Retarder OZ Amount Thickening Times Compressive Strength Initial Set 500psi 1000psi 80-90 NONE 5:00 - 6:00 8 hr 16 hr 24 hr 91-100 NONE 5:00 - 6:00 6 hr 11 hr 20 hr 101-110 NONE 5:00 - 6:00 6 hr 12 hr 19 hr 111-120 NONE 4:00 - 5:00 6 hr 10 hr 12 hr 121-130 NONE 4:00 - 5:00 4 hr 7 hr 10 hr 131-140 3 oz 4:00 - 5:00 4 hr 6 hr 7 hr 141-150 6 oz 4:00 - 5:00 6 hr 8 hr 10 hr 151-160 9 oz 4:00 - 5:00 8 hr 10 hr 12 hr 161-170 12 oz 4:00 - 5:00 9 hr 12 hr 14 hr 171-180 16 oz 4:00 - 5:00 9 hr 12 hr 14 hr 181-190 48 oz 4:00 - 5:00 10 hr 12 hr 15 hr 191-200 68 oz 4:00 - 5:00 8 hr 9 hr 10 hr 201-210 153 oz 4:00 - 5:00 10 hr 12 hr 13 hr

1-1-100 CEMENT ADDITIVE Retarder Field Data Sheet Retarder Formula YIELDS 4.0 BBLS (128 oz’s = 1 gal) DENSITY 16.2 PPG Example @ 190 deg F 63oz / 128 = 0.492 gal YIELD 1.09 FRESH WATER 100 gallons Fresh TEMPERATURE Retarder OZ Amount Thickening Times Compressive Strength Initial Set 500psi 2000psi 80-90 NONE 3:00 - 4:00 8 hr 16 hr 24 hr 91-100 13 oz 3:00 - 4:00 6 hr 12 hr 24 hr 101-110 27 oz 3:00 - 4:00 10 hr 12 hr 24 hr 111-120 32 oz 3:00 - 4:00 9 hr 11 hr 24 hr 121-130 37 oz 3:00 - 4:00 8 hr 12 hr 24 hr 131-140 40 oz 3:00 - 4:00 11 hr 13 hr 24 hr 141-150 63 oz 3:30 - 4:30 9 hr 12 hr 24 hr 151-160 63 oz 3:30 - 4:30 8 hr 10 hr 24 hr 161-170 63 oz 3:30 - 4:30 9 hr 12 hr 24 hr 171-180 63 oz 3:30 - 4:30 9 hr 12 hr 24 hr 181-190 63 oz 3:30 - 4:30 10 hr 12 hr 24 hr 191-200 68 oz 3:30 - 4:30 8 hr 12 hr 24 hr 201-210 153 oz 3:30 - 4:30 10 hr 12 hr 24 hr

# Text boxes

1 – 1 – 100 Additive Kit

Gas Stop Prevention

Squeeze Cementing

Coil Tubing Applications

Balanced Plugs

1 – 1 – 100 Additive Kit

Gas Stop Prevention

Squeeze Cementing

Coil Tubing Applications

Balanced Plugs